## Slide 1: Advanced Manufacturing Workflows for Tokamak Internal Components Commonwealth Fusion Systems CRADA
ORNL
Andrzej Nycz
Yukinori Yamamoto
Luke Meyer
Bill Carter
Chris Masuo
CFS
Brandon Sorbom
Cody Dennett
Shiyun Ruan
Jeremy Hollman
Deepthi Tammana
Moses Bloom

## Slide 2: Intro Video

## Slide 3: Advanced Manufacturing Workflows for Tokamak Internal Components
Objective: create and demonstrate workflow to build a component of the ARC vacuum vessel
Approach
  identify a group of suitable materials
  Select a component
  Create a testing workflow
  Demonstrate
  Down

## Slide 4: Materials: 316LMn Nitronic 50
Properties:
  As printed,
  Heat treated
Microstructure, Yield strength, Ultimate Tensile strength, Elongation, Reduction of Area, Charpy toughness, fracture toughness, microstructure

## Slide 5: Materials: 316LMn Nitronic 50
No major anisotropy in tensile strength
  45deg highest YS
No major effect on tensile strength from annealing
YS, UTS lower than wrought, EL higher

## Slide 6: First test part
Tokamak support leg test
Minimizing material waste
Workflow: defeature, toolpath, test print, final print
11.5” H, 17” L, 17” W. ~400lb
Model of the Support leg. Original part- left, defeatured model - right.
Toolpath visualization
Manufactured near net shape support leg.
Print direction

## Slide 7: Process development and controls
Nonstandard print direction
New process development
New process controls
Mechanical properties
Chart: Wire feed speed vs. Layer height
| 300 | 350 | 400 | 450 | 500
20 in/min | 1.5372 | 1.6512 | 1.7052 | 1.7954 | 1.8854
30 in/min | 1.37 | 1.3826 | 1.433 | 1.469 | 1.562
40 in/min | 1.227 | 1.277 | 1.3314 | 1.402 | 1.418
50 in/min | 1.166 | 1.212 | 1.2672 | 1.348 | 1.3564
60 in/min | 1.064 | 1.0794 | 1.094 | 1.2152 | 1.2278
Figure 14. Average layer height as a function of wire feed and print head speed
Print direction

## Slide 8: Concept test
Simplified geometry test
All previous concepts in action
3D Scan
Scan vs CAD 1.06mm – typical deviation
Scanned toroidal test component. Color representing deviation from the model.
Test part during the print (left) and the finished part (right).

## Slide 9: Toroidal part production
ORNL slicer Toolpath (left) and part cross section bead model (right).
316LMn – feedstock
Full workflow
3D scan
0.85 mm deviation
Model of the shield (left), defeatured part (middle), modeled part on the positioner.
Final part during manufacturing (left) and finished part (right).
Heatmap comparison of the printed part and the model (not to scale).

## Slide 10: Conclusions
Evaluated mechanical properties and selected materials: Nitronic 50, 316LMn
Workflow created
Process development
Demonstration of future manufacturing